# 保温管产品 SEO 内容（6 产品版）

版本说明： 本文件为 6 产品完整版，基于原有 3 产品版扩展，覆盖从经济型到高端认证型的完整产品线。每个产品独立页面，含 Meta 标签、详细描述、参数表、规格表和 FAQ。

标注说明： 标 \* 号者为行业典型值（非特定产品检测报告数据）。产品特定的热导率值（如 0.034、0.036 W/(m·K)）来自检测报告或产品数据表，直接引用不加 \*。

- 行业典型热导率：≤ 0.038 W/(m·K) at 0°C（闭孔 NBR/PVC 弹性体泡沫）\*

- 行业典型吸水率：≤ 5% (volume)\*

关键词来源：HVACR SEO 关键词表（1296+关键词，已验证竞品在用）。

GEO 优化说明：本内容同时覆盖 SEO（关键词布局）和 GEO（AI 引擎引用），通过结构化数据表、具体参数值、标准全称引用、FAQ 直接问答实现双重覆盖。

## Product 1: NBR/PVC B1 Economy (55 kg/m³)

### Meta Title (≤60 characters)

NBR/PVC B1 Insulation Tube Economy | AC Refrigeration

### Meta Description (≤155 characters)

Wholesale NBR/PVC B1 insulation tube for AC and refrigeration. Density 55 kg/m³, μ≥10000, 73 SKUs 1/4"–1-7/8". -40°C to +105°C. Low MOQ China supplier.

### 1. Product Name

NBR/PVC Rubber Foam Insulation Tube — B1 Fire Rated, Economy Grade (55 kg/m³)

### 2. Short Description

B1 fire rated NBR/PVC insulation tube for split AC, refrigeration, and chiller systems. Density 55 kg/m³, water vapour resistance μ ≥ 10,000. Available in black and blue. 73 SKUs covering 1/4" to 1-7/8" copper tube OD — the widest size range in our lineup. Two supplier sources for competitive pricing. Low MOQ, ready to ship.

### 3. Detailed Description

The most cost-effective insulation solution for standard AC and refrigeration piping. This NBR/PVC closed-cell foam tube provides reliable thermal insulation and condensation control at the lowest price point in our product range.

Dual supplier sourcing: Available from two manufacturers — Zhongjia Fulaosi (中嘉福乐斯) and Huamei (华美) — ensuring competitive pricing and stable supply. Both brands meet B1 (GB 8624) fire retardant requirements, with thermal conductivity as low as 0.033–0.034 W/(m·K) per test reports.

Widest size coverage: 73 SKUs spanning 1/4" to 1-7/8" (ID 6–48mm) with wall thickness options of 9mm, 13mm, 15mm, and 20mm. This is the broadest size range across all six product lines, covering everything from residential split AC to large commercial refrigeration.

Key Features:

• B1 flame retardant per GB 8624 — self-extinguishing, low smoke

• Closed-cell structure — prevents condensation and moisture ingress

• Water vapour resistance factor μ ≥ 10,000 — high moisture barrier performance

• Thermal conductivity: 0.033–0.034 W/(m·K) at 0°C (test report, brand-dependent)

• Water absorption ≤ 5%\* (volume)

• Oxygen index: 35.8% (ZJ brand) / ≥ 32% (HM brand) — high fire resistance

• 73 SKUs covering 1/4"~1-7/8" (ID 6–48mm) — widest size range in the lineup

• Pre-slit available upon request — no special tools needed for installation

Applications: Split AC pipe insulation, refrigeration cold lines, chiller and chilled water piping, cold rooms, heat pump systems, residential and light commercial HVAC.

### 4. Material & Standard

| Item | Detail |
| --- | --- |
| Material | NBR/PVC (Nitrile Butadiene Rubber / Polyvinyl Chloride) blended elastomeric foam |
| Structure | Closed-cell |
| Density | 55 kg/m³ |
| Fire Rating | B1 per GB 8624 (flame retardant) |
| Water Vapour Resistance Factor (μ) | ≥ 10,000 |
| Temperature Range | -40°C to +105°C |
| Thermal Conductivity | 0.033–0.034 W/(m·K) at 0°C (test report, brand-dependent) |
| Oxygen Index | 35.8% (ZJ brand) / ≥ 32% (HM brand) |
| Water Absorption | ≤ 5%\* (volume) |
| Available Colors | Black, Blue |
| Standard Length | 1.8m (9mm wall) / 2m (13mm, 15mm, 20mm wall) |
| Certifications | B1 (GB 8624) |

### 5. Specifications

Standard Lengths: 1.8m / 2m

| Copper Tube OD (Inch) | Insulation ID (mm) | Available Wall Thickness (mm) | Standard Length (m) |
| --- | --- | --- | --- |
| 1/4" | 6 | 9, 13, 15 | 1.8 / 2 |
| 3/8" | 10 | 9, 13, 15 | 1.8 / 2 |
| 1/2" | 13 | 9, 13, 15 | 1.8 / 2 |
| 5/8" | 16 | 9, 15, 20 | 1.8 / 2 |
| 3/4" | 19-20 | 9, 15, 20 | 1.8 / 2 |
| 7/8" | 22 | 20 | 2 |
| 1" | 25 | 9, 20 | 1.8 / 2 |
| 1-1/8" | 28 | 20 | 2 |
| 1-1/4" | 32-34 | 9, 20 | 1.8 / 2 |
| 1-1/2" | 38 | 20 | 2 |
| 1-5/8" | 43 | 9, 20 | 1.8 / 2 |
| 1-7/8" | 48 | 9, 20 | 1.8 / 2 |

Note: Wall thickness selection guide — 9mm for standard AC, 13–15mm for refrigeration, 20mm for deep freeze and low-temperature applications.

### 6. FAQ

Q: What is B1 fire rating?

A: B1 is a Chinese national standard (GB 8624) fire retardant classification. B1-rated materials are "difficult to ignite" — they self-extinguish when the flame source is removed and produce limited smoke. This is the standard fire rating required for HVAC insulation in most building applications.

Q: What is the difference between 55 kg/m³ and 65 kg/m³ density insulation?

A: Higher density (60–65 kg/m³) generally provides better thermal insulation performance due to a more compact cell structure. The 55 kg/m³ economy grade is sufficient for standard AC and refrigeration applications, while 60–65 kg/m³ grades are recommended for commercial and industrial applications requiring better insulation efficiency. Both share the same B1 fire rating and μ ≥ 10,000.

Q: What is the water vapour resistance factor μ?

A: The μ (mu) factor measures a material's ability to resist water vapour transmission. A higher μ value means better moisture barrier performance. Our insulation tubes have μ ≥ 10,000, classified as "high water vapour resistance" — essential for preventing condensation on cold refrigeration pipes.

## Product 2: NBR/PVC B1 High Density Standard Temp (60–65 kg/m³)

### Meta Title (≤60 characters)

NBR/PVC B1 High Density Insulation Tube | 60-65 kg/m³

### Meta Description (≤155 characters)

Wholesale high-density NBR/PVC B1 insulation tube. Density 60-65 kg/m³, μ≥10000, λ≤0.034. -40°C to +105°C. Blue. 7 SKUs. Low MOQ China supplier.

### 1. Product Name

NBR/PVC Rubber Foam Insulation Tube — B1 Fire Rated, High Density (60–65 kg/m³)

### 2. Short Description

Higher-density NBR/PVC B1 insulation tube for improved thermal performance. Density 60–65 kg/m³, water vapour resistance μ ≥ 10,000, thermal conductivity ≤ 0.034 W/(m·K). Temperature range -40°C to +105°C. Blue color. 7 SKUs covering 1/4" to 1-1/4". Low MOQ, ready to ship.

### 3. Detailed Description

An upgraded version of the economy grade, offering higher density (60–65 kg/m³) for better insulation performance within the same standard temperature range (-40°C to +105°C).

Why higher density? In closed-cell NBR/PVC foam, higher density means a more compact cell structure with smaller, more uniform air pockets. This reduces convective heat transfer within the cells, resulting in lower thermal conductivity (≤ 0.034 W/(m·K) per test report) compared to the 55 kg/m³ economy grade. The denser material also offers better mechanical durability and tear resistance during installation.

Same temp range, better performance: While the temperature range remains -40°C to +105°C (same as the economy grade), the higher density provides a measurable improvement in thermal insulation efficiency — making it suitable for applications where the economy grade meets the temperature requirement but enhanced insulation performance is desired.

Key Features:

• B1 flame retardant per GB 8624 — self-extinguishing, low smoke

• Closed-cell structure — prevents condensation and moisture ingress

• Water vapour resistance factor μ ≥ 10,000 — high moisture barrier performance

• Thermal conductivity: ≤ 0.034 W/(m·K) at 0°C (test report) — outperforms industry typical ≤ 0.038 W/(m·K)\*

• Water absorption ≤ 5%\* (volume)

• Oxygen index ≥ 32% — high fire resistance

• Higher density (60–65 kg/m³) for improved insulation performance vs 55 kg/m³ economy grade

• Blue color for easy identification of higher-density insulation lines

Applications: Commercial AC systems, refrigeration cold lines, chiller piping, cold rooms, heat pump systems — where standard temperature range is sufficient but enhanced insulation performance is preferred.

### 4. Material & Standard

| Item | Detail |
| --- | --- |
| Material | NBR/PVC (Nitrile Butadiene Rubber / Polyvinyl Chloride) blended elastomeric foam |
| Structure | Closed-cell |
| Density | 60–65 kg/m³ |
| Fire Rating | B1 per GB 8624 (flame retardant) |
| Water Vapour Resistance Factor (μ) | ≥ 10,000 |
| Temperature Range | -40°C to +105°C |
| Thermal Conductivity | ≤ 0.034 W/(m·K) at 0°C (test report) |
| Oxygen Index | ≥ 32% |
| Water Absorption | ≤ 5%\* (volume) |
| Color | Blue |
| Standard Length | 1.8m (9mm wall) / 2m (15mm wall) |
| Certifications | B1 (GB 8624) |

### 5. Specifications

Standard Lengths: 1.8m / 2m

| Copper Tube OD (Inch) | Insulation ID (mm) | Available Wall Thickness (mm) | Standard Length (m) |
| --- | --- | --- | --- |
| 1/4" | 6 | 9 | 1.8 |
| 3/8" | 10 | 9 | 1.8 |
| 1/2" | 13 | 9 | 1.8 |
| 5/8" | 16 | 15 | 2 |
| 3/4" | 20 | 15 | 2 |
| 1" | 25 | 15 | 2 |
| 1-1/4" | 32 | 15 | 2 |

Note: 7 SKUs. Wall thickness selection guide — 9mm for standard AC, 15mm for refrigeration and cold lines.

### 6. FAQ

Q: Why choose higher density (60–65 kg/m³) insulation?

A: Higher density foam has a more compact closed-cell structure, which reduces convective heat transfer within the cells and results in lower thermal conductivity. The test report confirms ≤ 0.034 W/(m·K) for this grade, compared to 0.033–0.034 W/(m·K) for the 55 kg/m³ economy grade. Higher density also provides better mechanical durability and tear resistance during installation.

Q: How does this differ from the economy grade (Product 1)?

A: Both products share the same B1 fire rating (GB 8624), μ ≥ 10,000, and temperature range (-40°C to +105°C). The key differences are: density (60–65 kg/m³ vs 55 kg/m³), color (blue only vs black and blue), SKU count (7 vs 73), and size range (1/4"~1-1/4" vs 1/4"~1-7/8"). The higher density grade offers better insulation performance but in a more focused size range.

Q: Does higher density mean better insulation at the same temperature range?

A: Yes. While both products operate within -40°C to +105°C, the higher density (60–65 kg/m³) provides lower thermal conductivity (≤ 0.034 W/(m·K) per test report), meaning less heat transfer through the insulation for the same wall thickness. This translates to better energy efficiency and condensation control, particularly important for refrigeration cold lines.

## Product 3: NBR/PVC B1 High Density Extended Temp (60–65 kg/m³)

### Meta Title (≤60 characters)

NBR/PVC B1 Extended Temp Insulation Tube | -50°C +110°C

### Meta Description (≤155 characters)

Extended temp NBR/PVC B1 insulation tube. -50°C to +110°C, μ≥10000. UL94, CE, REACH, RoHS certified. Blue. 7 SKUs 1/4"-1-1/4". Low MOQ China supplier.

### 1. Product Name

NBR/PVC Rubber Foam Insulation Tube — B1 Fire Rated, High Density, Extended Temperature (60–65 kg/m³)

### 2. Short Description

Extended temperature NBR/PVC B1 insulation tube for deep freeze and high-temperature applications. Temperature range -50°C to +110°C, water vapour resistance μ ≥ 10,000. Multi-certified: BS476, UL94, CE, REACH, RoHS. Blue color. 7 SKUs covering 1/4" to 1-1/4". Low MOQ, ready to ship.

### 3. Detailed Description

For applications that exceed the standard temperature range of -40°C to +105°C. This product extends the operating range to -50°C on the low end and +110°C on the high end, making it suitable for deep freeze systems and high-temperature process piping.

Extended low temperature (-50°C): Standard NBR/PVC insulation is rated to -40°C. This product's formulation maintains flexibility and thermal performance down to -50°C, making it suitable for low-temperature freezer rooms, blast freezers, and industrial process cooling where pipe surfaces can drop below -40°C.

Extended high temperature (+110°C): The upper limit is raised from +105°C to +110°C, accommodating hot gas lines and high-temperature refrigerant piping in heat pump and industrial systems.

Multi-certified for international projects: In addition to B1 (GB 8624) and BS476, this product carries UL94, CE, REACH, and RoHS certifications — enabling compliance with fire safety, electrical, environmental, and chemical regulations across multiple international markets.

Key Features:

• B1 flame retardant per GB 8624 — self-extinguishing, low smoke

• Closed-cell structure — prevents condensation and moisture ingress

• Water vapour resistance factor μ ≥ 10,000 — high moisture barrier performance

• Thermal conductivity: 0.036 W/(m·K) at 0°C (test report)

• Water absorption ≤ 5%\* (volume)

• Extended temperature range: -50°C to +110°C — for deep freeze and high-temperature applications

• Oxygen index: 36.2% — superior fire resistance

• Multi-certified: BS476, UL94, CE, REACH, RoHS — for international project compliance

Applications: Blast freezers, low-temperature cold rooms, industrial process cooling, hot gas lines, heat pump systems, refrigeration systems requiring international certifications — pharmaceutical, food processing, export projects.

### 4. Material & Standard

| Item | Detail |
| --- | --- |
| Material | NBR/PVC (Nitrile Butadiene Rubber / Polyvinyl Chloride) blended elastomeric foam |
| Structure | Closed-cell |
| Density | 60–65 kg/m³ |
| Fire Rating | B1 per GB 8624 (flame retardant) |
| Applicable Standards | GB 8624, BS476 |
| Water Vapour Resistance Factor (μ) | ≥ 10,000 |
| Temperature Range | -50°C to +110°C |
| Thermal Conductivity | 0.036 W/(m·K) at 0°C (test report) |
| Oxygen Index | 36.2% |
| Water Absorption | ≤ 5%\* (volume) |
| Color | Blue |
| Standard Length | 1.8m (9mm wall) / 2m (15mm wall) |
| Certifications | BS476, UL94, CE, REACH, RoHS |

### 5. Specifications

Standard Lengths: 1.8m / 2m

| Copper Tube OD (Inch) | Insulation ID (mm) | Available Wall Thickness (mm) | Standard Length (m) |
| --- | --- | --- | --- |
| 1/4" | 6 | 9 | 1.8 |
| 3/8" | 10 | 9 | 1.8 |
| 1/2" | 13 | 9 | 1.8 |
| 5/8" | 16 | 15 | 2 |
| 3/4" | 20 | 15 | 2 |
| 1" | 25 | 15 | 2 |
| 1-1/4" | 32 | 15 | 2 |

Note: 7 SKUs. Same size range as Product 2, but with extended temperature range and international certifications.

### 6. FAQ

Q: What is the extended temperature range (-50°C to +110°C) for?

A: The extended range covers applications that exceed standard NBR/PVC limits (-40°C to +105°C). The -50°C low end is for deep freeze systems such as blast freezers, low-temperature cold rooms, and industrial process cooling where pipe surfaces can drop below -40°C. The +110°C high end accommodates hot gas lines and high-temperature refrigerant piping in heat pump and industrial systems.

Q: What do the certifications (UL94, CE, REACH, RoHS) mean?

A: UL94 is a US standard for flammability of plastic materials. CE marking indicates conformity with European health, safety, and environmental standards. REACH ensures compliance with EU chemical registration requirements. RoHS restricts hazardous substances in electrical and electronic equipment. Together, these certifications enable the product to be specified in projects across North America, Europe, and other regulated markets.

Q: How does this differ from the standard high-density version (Product 2)?

A: Both share the same density (60–65 kg/m³), B1 fire rating, μ ≥ 10,000, and size range (1/4"~1-1/4", 7 SKUs). The key differences are: temperature range (-50°C~+110°C vs -40°C~+105°C), oxygen index (36.2% vs ≥ 32%), thermal conductivity (0.036 vs ≤ 0.034 W/(m·K)), and certifications (BS476 + UL94 + CE + REACH + RoHS vs B1 only). Product 3 is for applications requiring extended temperatures or international compliance.

## Product 4: NBR/PVC Class 0 Fire Rated (60–65 kg/m³, Red)

### Meta Title (≤60 characters)

Class 0 NBR/PVC Insulation Tube Red | BS476 Fire Rated

### Meta Description (≤155 characters)

Class 0 NBR/PVC insulation tube. BS476 Part 6+7, B1 GB8624. Red, -50°C to +110°C, μ≥10000. UL94, CE, REACH, RoHS. 7 SKUs. Low MOQ China supplier.

### 1. Product Name

NBR/PVC Rubber Foam Insulation Tube — Class 0 Fire Rated, BS476 Certified (Red)

### 2. Short Description

Class 0 fire rated NBR/PVC insulation tube with BS476 Part 6 (Class 0) and Part 7 (Class 1) certification, also complying with B1 (GB 8624). Density 60–65 kg/m³, temperature range -50°C to +110°C, μ ≥ 10,000. Red color for easy identification of fire-rated lines. Multi-certified: BS476, UL94, CE, REACH, RoHS. 7 SKUs covering 1/4" to 1". Low MOQ, ready to ship.

### 3. Detailed Description

The highest fire safety rating available in our NBR/PVC insulation range. This product meets Class 0 under BS476 Part 6 (fire propagation) and Class 1 under BS476 Part 7 (surface spread of flame) — the most stringent fire performance classifications under UK standards — while also complying with B1 (GB 8624).

Class 0 — the UK fire standard: Class 0 is the highest fire performance classification under the UK building regulations, achieved by passing both BS476 Part 6 (fire propagation index) and Part 7 (surface spread of flame). It is required in specific building types including high-rise residential, hospitals, schools, and escape routes. Products meeting Class 0 typically also satisfy B1 (GB 8624) requirements.

Red color for safety identification: The red color allows easy visual identification of fire-rated insulation lines during installation and inspection. On job sites with multiple insulation grades, color coding helps inspectors and engineers quickly verify that the correct fire-rated material has been installed in critical areas.

For critical infrastructure: Multi-certified with BS476, UL94, CE, REACH, and RoHS, this product is engineered for commercial buildings, hospitals, marine and offshore applications, and any project where UK/BS fire certification is specified.

Key Features:

• Class 0 (BS476 Part 6) + Class 1 (BS476 Part 7) + B1 (GB 8624) — triple fire certified, highest fire safety in NBR/PVC range

• Closed-cell structure — prevents condensation and moisture ingress

• Water vapour resistance factor μ ≥ 10,000 — high moisture barrier performance

• Thermal conductivity: ≤ 0.036 W/(m·K) at 0°C (test report)

• Water absorption ≤ 5%\* (volume)

• Oxygen index ≥ 36% — superior fire resistance

• Red color for visual identification of fire-rated lines on job sites

• Multi-certified: BS476, UL94, CE, REACH, RoHS — for UK, Commonwealth, and Middle East compliance

Applications: Commercial buildings, hospitals, schools, data centres, marine and offshore HVAC, district cooling — anywhere UK/BS fire certification is specified or where the highest level of fire performance is required.

### 4. Material & Standard

| Item | Detail |
| --- | --- |
| Material | NBR/PVC (Nitrile Butadiene Rubber / Polyvinyl Chloride) blended elastomeric foam |
| Structure | Closed-cell |
| Density | 60–65 kg/m³ |
| Fire Rating | Class 0 (BS476 Part 6) + Class 1 (BS476 Part 7) + B1 (GB 8624) |
| Applicable Standards | BS476, GB 8624 |
| Water Vapour Resistance Factor (μ) | ≥ 10,000 |
| Temperature Range | -50°C to +110°C |
| Thermal Conductivity | ≤ 0.036 W/(m·K) at 0°C (test report) |
| Oxygen Index | ≥ 36% |
| Water Absorption | ≤ 5%\* (volume) |
| Color | Red |
| Standard Length | 1.8m (9mm wall) / 2m (10mm, 15mm, 20mm wall) |
| Certifications | BS476, UL94, CE, REACH, RoHS |

### 5. Specifications

Standard Lengths: 1.8m / 2m

| Copper Tube OD (Inch) | Insulation ID (mm) | Wall Thickness (mm) | Standard Length (m) |
| --- | --- | --- | --- |
| 1/4" | 6 | 15 | 2 |
| 3/8" | 10 | 15 | 2 |
| 1/2" | 13 | 15 | 2 |
| 5/8" | 16 | 20 | 2 |
| 3/4" | 20 | 20 | 2 |
| 1" | 25 | 9 | 1.8 |
| 1" | 25 | 10 | 2 |

Note: 7 SKUs. Class 0 grade is available in select sizes. For sizes not listed, please contact us for availability and custom production options.

### 6. FAQ

Q: What is Class 0 fire rating?

A: Class 0 is the highest fire performance classification under UK building regulations (BS476). It requires passing two tests: BS476 Part 6 (fire propagation — measuring heat release and spread) and BS476 Part 7 (surface spread of flame — Class 1 rating). Class 0 is required in specific building types including high-rise residential, hospitals, schools, and escape routes. It is recognized in UK, Commonwealth, and Middle East markets.

Q: What is the difference between Class 0 and B1?

A: Class 0 (BS476) and B1 (GB 8624) are from different national standards. Class 0 is the UK standard's highest fire performance rating, recognized in UK, Commonwealth, and Middle East markets. B1 is the Chinese standard's flame retardant rating. Class 0 is more stringent — products meeting Class 0 typically also comply with B1 requirements, but the reverse is not necessarily true. This product meets both standards for dual-market compliance.

Q: Why is this product red?

A: The red color serves as a visual identifier for premium fire-rated insulation lines. On job sites with multiple insulation grades, color coding helps inspectors and engineers quickly verify that the correct fire-rated material has been installed in critical areas such as escape routes, plant rooms, and fire compartments. The red color does not affect the insulation's thermal or mechanical properties.

## Product 5: NBR Lightweight (≤ 50 kg/m³, Black)

### Meta Title (≤60 characters)

NBR Lightweight Insulation Tube ≤50 kg/m³ | GREENGUARD

### Meta Description (≤155 characters)

Lightweight pure NBR insulation tube ≤50 kg/m³. GREENGUARD Gold, EPD certified. -50°C to +105°C, μ≥10000. Black. 8 SKUs. Low MOQ China supplier.

### 1. Product Name

NBR Rubber Foam Insulation Tube — Lightweight Grade, Pure NBR (≤ 50 kg/m³)

### 2. Short Description

Lightweight pure NBR insulation tube for superior flexibility and thermal efficiency. Density ≤ 50 kg/m³, water vapour resistance μ ≥ 10,000. GREENGUARD Gold and EPD certified for indoor air quality and green building compliance. Temperature range -50°C to +105°C. Black color. 8 SKUs covering 1/4" to 1-1/4". Low MOQ, ready to ship.

### 3. Detailed Description

Unlike standard NBR/PVC blends, this product is manufactured from pure NBR foam — no PVC. The result: lower density (≤ 50 kg/m³), superior flexibility, and better thermal insulation efficiency.

Why lower density is better: In closed-cell foam insulation, lower density means more trapped air cells per unit volume. Since still air is one of the best thermal insulators, lower density directly translates to better insulation performance. A density of ≤ 50 kg/m³ is considered premium grade, compared to standard grades at 55–65 kg/m³. The thermal conductivity of 0.036 W/(m·K) per product data confirms excellent thermal efficiency at this density.

Pure NBR vs NBR/PVC: Pure NBR (nitrile butadiene rubber) foam is manufactured without PVC blending, resulting in superior flexibility, better ozone and weathering resistance, and a softer feel that makes installation easier around bends and fittings. NBR/PVC blends are more common and cost-effective, while pure NBR is typically used in premium applications.

GREENGUARD Gold certified: This product carries GREENGUARD Gold certification, the most stringent indoor air quality certification, ensuring low chemical emissions for use in sensitive environments such as schools, healthcare facilities, and clean rooms. The EPD (Environmental Product Declaration) provides transparent environmental impact data for green building projects pursuing LEED or BREEAM certification.

Key Features:

• Pure NBR (no PVC) — superior flexibility and ozone resistance

• Closed-cell structure — prevents condensation and moisture ingress

• Water vapour resistance factor μ ≥ 10,000 — high moisture barrier performance

• Lowest density ≤ 50 kg/m³ — maximum thermal efficiency (more trapped air cells per unit volume)

• Thermal conductivity: 0.036 W/(m·K) at 0°C (product data)

• Water absorption ≤ 5%\* (volume)

• GREENGUARD Gold certified — for indoor air quality and sensitive environments

• EPD certified — environmental product declaration for green building projects

Applications: Pharmaceutical and food industry refrigeration, clean rooms, hospitals, schools, district cooling, marine HVAC, indoor air quality sensitive projects, green building certified projects (LEED, BREEAM).

### 4. Material & Standard

| Item | Detail |
| --- | --- |
| Material | NBR (Nitrile Butadiene Rubber) — pure elastomeric foam, non-PVC |
| Structure | Closed-cell |
| Density | ≤ 50 kg/m³ |
| Fire Rating | Class 1 (BS476 Part 7) + B1 (GB 8624) |
| Applicable Standards | BS476, GB 8624 |
| Water Vapour Resistance Factor (μ) | ≥ 10,000 |
| Temperature Range | -50°C to +105°C |
| Thermal Conductivity | 0.036 W/(m·K) at 0°C (product data) |
| Oxygen Index | Not available |
| Water Absorption | ≤ 5%\* (volume) |
| Color | Black |
| Standard Length | 2m |
| Certifications | GREENGUARD Gold, EPD |

### 5. Specifications

Standard Length: 2m

| Copper Tube OD (Inch) | Insulation ID (mm) | Wall Thickness (mm) | Standard Length (m) |
| --- | --- | --- | --- |
| 1/4" | 6 | 14 | 2 |
| 3/8" | 10 | 14 | 2 |
| 1/2" | 13 | 14 | 2 |
| 5/8" | 16 | 14 | 2 |
| 3/4" | 20 | 14 | 2 |
| 7/8" | 22 | 20 | 2 |
| 1" | 25 | 10 | 2 |
| 1-1/4" | 32 | 10 | 2 |

Note: 8 SKUs. Wall thickness 14mm is unique to this lightweight NBR grade, optimized for the lower-density material to maintain equivalent thermal performance.

### 6. FAQ

Q: What is the difference between pure NBR and NBR/PVC insulation?

A: Pure NBR (nitrile butadiene rubber) foam is manufactured without PVC blending, resulting in lower density (≤ 50 kg/m³ vs 55–65 kg/m³ for NBR/PVC), superior flexibility, and better ozone and weathering resistance. NBR/PVC blends are more common and cost-effective, while pure NBR is typically used in premium applications requiring higher performance, better flexibility, or specific certifications such as GREENGUARD Gold.

Q: Why is lower density better for insulation?

A: In closed-cell foam insulation, lower density means more trapped air cells per unit volume. Since still air is one of the best thermal insulators, lower density foam generally provides better thermal insulation performance (lower thermal conductivity). A density of ≤ 50 kg/m³ is considered premium grade, compared to standard grades at 55–65 kg/m³. This product's thermal conductivity of 0.036 W/(m·K) per product data confirms excellent thermal efficiency.

Q: What is GREENGUARD Gold certification?

A: GREENGUARD Gold is the most stringent indoor air quality certification by UL (Underwriters Laboratories). It sets the lowest emission limits for volatile organic compounds (VOCs) and other chemicals, making it suitable for sensitive environments such as schools, healthcare facilities, and clean rooms. Products with GREENGUARD Gold certification contribute to LEED credit for low-emitting materials. This product also carries an EPD (Environmental Product Declaration) for green building projects.

## Product 6: NBR Multi-Certified Premium (Blue)

### Meta Title (≤60 characters)

NBR Premium Insulation Tube Class 0 | FM 4924 UL94 V-0

### Meta Description (≤155 characters)

Premium NBR insulation tube. Class 0+1+B1, FM 4924, UL94 V-0, GREENGUARD Gold. -50°C to +105°C, μ≥10000. Blue. 10 SKUs. Low MOQ China supplier.

### 1. Product Name

NBR Rubber Foam Insulation Tube — Multi-Certified Premium Grade (Triple Fire Certified)

### 2. Short Description

Premium pure NBR insulation tube with triple fire certification: Class 0 (BS476 Part 6) + Class 1 (BS476 Part 7) + B1 (GB 8624). FM 4924 and UL94 V-0 certified for critical applications. GREENGUARD Gold for indoor air quality. Temperature range -50°C to +105°C, μ ≥ 10,000. Blue color. 10 SKUs covering 1/4" to 1-1/4". Low MOQ, ready to ship.

### 3. Detailed Description

The top-tier product in our insulation range — engineered for critical applications where the highest level of fire safety, international certification, and premium brand quality are required.

Triple fire certified: This product carries the most comprehensive fire certification in our lineup: Class 0 (BS476 Part 6 — fire propagation), Class 1 (BS476 Part 7 — surface spread of flame), and B1 (GB 8624). This triple certification ensures compliance with fire codes across UK, Commonwealth, Middle East, and Chinese markets.

FM 4924 — for critical applications: Factory Mutual (FM) 4924 is the approval standard for clean room fire suppression materials. FM 4924 certification means this product has been tested and approved for use in environments where fire suppression is critical, such as data centres, semiconductor fabrication facilities, and pharmaceutical clean rooms.

UL94 V-0 — highest UL flame rating: UL94 V-0 is the highest flame rating under the UL94 standard for plastic materials. V-0 rated materials self-extinguish within 10 seconds after flame removal, with no flaming drips — critical for electrical and electronic equipment enclosures.

Premium brand quality: Manufactured by Armaflex/Fulaosi (阿乐斯/福乐斯), a globally recognized premium insulation brand, ensuring consistent quality, long service life (typically 20+ years), and reliable performance in demanding applications.

Key Features:

• Pure NBR (no PVC) — superior flexibility and ozone resistance

• Closed-cell structure — prevents condensation and moisture ingress

• Water vapour resistance factor μ ≥ 10,000 — high moisture barrier performance

• Triple fire certified: Class 0 (BS476 Part 6) + Class 1 (BS476 Part 7) + B1 (GB 8624)

• Thermal conductivity: 0.036 W/(m·K) at 0°C (product data)

• Water absorption ≤ 5%\* (volume)

• FM 4924 certified — for critical applications requiring factory mutual approval

• UL94 V-0 rated — highest UL flame rating for plastic materials

Applications: Data centres, semiconductor fabrication facilities, pharmaceutical clean rooms, hospitals, marine and offshore HVAC, critical infrastructure — projects requiring the highest level of fire safety and multi-standard certification.

### 4. Material & Standard

| Item | Detail |
| --- | --- |
| Material | NBR (Nitrile Butadiene Rubber) — pure elastomeric foam, non-PVC |
| Structure | Closed-cell |
| Density | Not specified (premium grade) |
| Fire Rating | Class 0 (BS476 Part 6) + Class 1 (BS476 Part 7) + B1 (GB 8624) |
| Applicable Standards | BS476, GB 8624 |
| Water Vapour Resistance Factor (μ) | ≥ 10,000 |
| Temperature Range | -50°C to +105°C |
| Thermal Conductivity | 0.036 W/(m·K) at 0°C (product data) |
| Oxygen Index | Not available |
| Water Absorption | ≤ 5%\* (volume) |
| Color | Blue |
| Standard Length | 2m |
| Certifications | FM 4924, UL94 V-0, GREENGUARD Gold |

### 5. Specifications

Standard Length: 2m

| Copper Tube OD (Inch) | Insulation ID (mm) | Wall Thickness (mm) | Standard Length (m) |
| --- | --- | --- | --- |
| 1/4" | 6 | 15 | 2 |
| 3/8" | 10 | 15 | 2 |
| 1/2" | 13 | 15 | 2 |
| 5/8" | 16 | 15 | 2 |
| 3/4" | 20 | 15 | 2 |
| 7/8" | 22 | 20 | 2 |
| 1" | 25 | 10 | 2 |
| 1" | 25 | 20 | 2 |
| 1-1/8" | 28 | 20 | 2 |
| 1-1/4" | 32 | 10 | 2 |

Note: 10 SKUs — the most comprehensive size range among pure NBR products. 1" available in two wall thickness options (10mm and 20mm) for standard and heavy-duty applications.

### 6. FAQ

Q: What is FM 4924 certification?

A: FM 4924 is the Factory Mutual approval standard for clean room fire suppression materials. It evaluates materials for fire performance in environments where fire suppression is critical — such as data centres, semiconductor fabrication facilities, and pharmaceutical clean rooms. FM 4924 certification indicates that the material has been tested and approved for use in these sensitive environments where even a small fire could cause catastrophic damage.

Q: How does this differ from the lightweight NBR (Product 5)?

A: Both are pure NBR (no PVC) with μ ≥ 10,000, temperature range -50°C to +105°C, and thermal conductivity of 0.036 W/(m·K). The key differences are: fire rating (Class 0 + Class 1 + B1 triple certified vs Class 1 + B1), color (blue vs black), density (not specified vs ≤ 50 kg/m³), SKU count (10 vs 8), and certifications (FM 4924 + UL94 V-0 + GREENGUARD Gold vs GREENGUARD Gold + EPD). Product 6 offers the highest fire safety and critical application certifications.

Q: When should I choose this product over other options?

A: Choose Product 6 when your project requires: (1) Class 0 fire rating under BS476 — for UK, Commonwealth, or Middle East compliance; (2) FM 4924 approval — for data centres, clean rooms, or critical infrastructure; (3) UL94 V-0 — for electrical and electronic applications; (4) premium brand quality from a globally recognized manufacturer. For standard AC and refrigeration, Products 1–3 are more cost-effective. For green building projects requiring GREENGUARD Gold but not Class 0, Product 5 is sufficient.

## 附：6 产品对比总表

| Parameter | P1: B1 Economy | P2: B1 High Density | P3: B1 Extended Temp | P4: Class 0 Red | P5: NBR Lightweight | P6: NBR Premium |
| --- | --- | --- | --- | --- | --- | --- |
| Material | NBR/PVC | NBR/PVC | NBR/PVC | NBR/PVC | Pure NBR | Pure NBR |
| Fire Rating | B1 (GB 8624) | B1 (GB 8624) | B1 (GB 8624) | Class 0 + Class 1 (BS476) + B1 | Class 1 (BS476 P7) + B1 | Class 0 + Class 1 (BS476) + B1 |
| Density | 55 kg/m³ | 60–65 kg/m³ | 60–65 kg/m³ | 60–65 kg/m³ | ≤ 50 kg/m³ | Not specified |
| Temp Range | -40°C ~ +105°C | -40°C ~ +105°C | -50°C ~ +110°C | -50°C ~ +110°C | -50°C ~ +105°C | -50°C ~ +105°C |
| μ | ≥ 10,000 | ≥ 10,000 | ≥ 10,000 | ≥ 10,000 | ≥ 10,000 | ≥ 10,000 |
| Thermal Conductivity | 0.033–0.034 W/(m·K) | ≤ 0.034 W/(m·K) | 0.036 W/(m·K) | ≤ 0.036 W/(m·K) | 0.036 W/(m·K) | 0.036 W/(m·K) |
| Colors | Black, Blue | Blue | Blue | Red | Black | Blue |
| Size Range (ID) | 6–48mm (1/4"~1-7/8") | 6–32mm (1/4"~1-1/4") | 6–32mm (1/4"~1-1/4") | 6–25mm (1/4"~1") | 6–32mm (1/4"~1-1/4") | 6–32mm (1/4"~1-1/4") |
| Wall Thickness Options | 9, 13, 15, 20mm | 9, 15mm | 9, 15mm | 9, 10, 15, 20mm | 10, 14, 20mm | 10, 15, 20mm |
| Standard Length | 1.8m / 2m | 1.8m / 2m | 1.8m / 2m | 1.8m / 2m | 2m | 2m |
| SKU Count | 73 | 7 | 7 | 7 | 8 | 10 |
| Certifications | B1 (GB 8624) | B1 (GB 8624) | BS476, UL94, CE, REACH, RoHS | BS476, UL94, CE, REACH, RoHS | GREENGUARD Gold, EPD | FM 4924, UL94 V-0, GREENGUARD Gold |
| Best For | Standard AC & refrigeration, widest size range, most cost-effective | Higher density for better insulation, same temp range | Deep freeze (-50°C) & high temp (+110°C), international projects | Highest fire safety (Class 0), commercial buildings, hospitals, marine | Lightweight, indoor air quality, GREENGUARD Gold, green building | Critical applications, FM 4924, premium brand, top-tier fire safety |

## 附：SEO 关键词使用说明

以上内容已自然融入以下高价值关键词（来源：1296+关键词表，已验证竞品在用）：

Product 1 (B1 Economy, 55 kg/m³):

NBR insulation tube, rubber insulation tube, NBR/PVC insulation pipe, refrigeration insulation tube, AC insulation tube, elastomeric insulation tube, rubber pipe insulation, NBR insulation tube supplier, rubber insulation manufacturer, wholesale insulation tube, NBR insulation tube 1/2 3/4 1 inch, B1 fire rated insulation, insulation tube 13mm 19mm 25mm, NBR insulation density 55 kg/m3, HVAC insulation tube, insulation tube for air conditioning, AC pipe insulation, refrigeration pipe insulation, chiller pipe insulation, low cost insulation tube

Product 2 (B1 High Density, 60–65 kg/m³):

NBR insulation tube, rubber insulation tube, NBR/PVC insulation pipe, high density insulation tube, B1 fire rated insulation, refrigeration insulation tube, HVAC insulation tube, insulation tube for air conditioning, NBR insulation density 60-65 kg/m3, wholesale insulation tube, elastomeric insulation tube, NBR insulation tube supplier, AC pipe insulation, chiller pipe insulation, blue insulation tube

Product 3 (B1 Extended Temp, 60–65 kg/m³):

NBR insulation tube, rubber insulation tube, NBR/PVC insulation pipe, extended temperature insulation, deep freeze insulation, UL94 insulation tube, CE certified insulation, REACH insulation, RoHS insulation, HVAC insulation tube, refrigeration pipe insulation, -50°C insulation, high temperature insulation, BS476 insulation, elastomeric insulation tube, wholesale insulation tube

Product 4 (Class 0 Red, 60–65 kg/m³):

NBR insulation tube, rubber insulation tube, NBR/PVC insulation pipe, Class 0 insulation tube, BS476 insulation, fire rated insulation, red insulation tube, UL94 insulation tube, CE certified insulation, REACH insulation, RoHS insulation, marine insulation, hospital insulation, commercial building insulation, NBR/PVC insulation Class 0 Class 1, elastomeric insulation tube, wholesale insulation tube

Product 5 (NBR Lightweight, ≤ 50 kg/m³):

NBR insulation tube, elastomeric insulation tube, rubber insulation tube, pure NBR insulation, lightweight insulation tube, GREENGUARD insulation, EPD insulation, low density insulation, NBR insulation density 50 kg/m3, indoor air quality insulation, HVAC insulation tube, insulation tube for air conditioning, closed cell insulation, NBR insulation manufacturer, wholesale insulation tube, LEED insulation, BREEAM insulation

Product 6 (NBR Premium, Multi-Certified):

NBR insulation tube, elastomeric insulation tube, rubber insulation tube, Class 0 insulation tube, FM 4924 insulation, UL94 V-0 insulation, GREENGUARD insulation, premium insulation tube, fire rated insulation, NBR insulation tube supplier, critical application insulation, data centre insulation, clean room insulation, NBR/PVC insulation Class 0 Class 1, wholesale insulation tube, Armaflex insulation, closed cell insulation

## 附：GEO 优化要点

本内容针对 AI 生成式搜索引擎（ChatGPT、Perplexity、Google AI Overviews）做了以下优化：

1. 结构化数据表 — 所有参数以表格形式呈现，AI 引擎可直接解析引用。6 个产品的 Material & Standard 表和 Specifications 表提供完整的结构化参数。

2. 具体参数值 — 密度、温度范围、μ 值、热导率、氧指数均给出精确数字，不使用"高""低"等模糊描述。产品特定值（如 0.034、0.036 W/(m·K)）与行业典型值（≤ 0.038 W/(m·K)\*）明确区分。

3. 标准全称引用 — 写明 "BS476 Part 6 (fire propagation)" 而非仅 "Class 0"；写明 "GB 8624" 而非仅 "B1"；写明 "FM 4924 (Factory Mutual approval standard for clean room fire suppression)" 而非仅 "FM 4924"。便于 AI 引擎交叉验证。

4. 6 产品对比总表 — 13 项参数 × 6 产品的完整对比矩阵，直接回答"不同保温管有什么区别""哪个产品适合什么场景"类查询。

5. FAQ 直接问答 — 每个产品 2–3 个 FAQ，以问答形式直接回答买家常见问题。AI 引擎优先抓取 FAQ 格式内容，尤其是"What is Class 0""What is FM 4924""What is GREENGUARD Gold"等定义类查询。

6. 层次化标题 — H2（产品级）/ H3（字段级）清晰分层，AI 引擎可按段落精确引用。

7. 产品间交叉引用 — FAQ 中明确说明产品间的差异（如 Product 3 vs Product 2、Product 6 vs Product 5），帮助 AI 引擎理解产品定位和选型逻辑。

8. 认证全称展开 — 所有认证（UL94, CE, REACH, RoHS, GREENGUARD Gold, EPD, FM 4924）在首次出现时附上完整说明，便于 AI 引擎建立认证与产品属性的关联。

\* 行业典型值 for closed-cell NBR/PVC elastomeric foam; not from a specific product test report. Product-specific thermal conductivity values (e.g., 0.033, 0.034, 0.036 W/(m·K)) are from test reports or product data sheets.

本内容由 Coze AI 生成，请遵循相关法律法规及《人工智能生成合成内容标识办法》使用与传播。